GALVANIZED STEEL LIGHTING STANDARDS

The Standard Specifications are revised as follows:

SECTION 913, BEGIN LINE 1089, INSERT AS FOLLOWS:

4. Galvanized Steel Lighting Standards. The pole and base plate shall be fabricated from steel in accordance with ASTM A 572M (ASTM A 572), or A 595, or A 1011 with

a minimum yield of 345 MPa (50,000 psi). Single member mast arms and the upper