HMA SMOOTHNESS

The Standard Specifications are revised as follows:

SECTION 401, DELETE LINES 574 THROUGH 574aa.

SECTION 401, AFTER LINE 575, INSERT AS FOLLOWS:

| ADJUSTMENT FOR SMOOTHNESS (PI0.0) ZERO BLANKING BAND |
| --- |
| Design Speed Greater Than 45 mph (70 km/hr) |
| Profile Index in./0.1 mi. (mm per 0.16 km) | Pay Factor |
| Over 0.00 to 1.20 in. (Over 0 to 30 mm) | 1.06 |
| Over 1.20 to 1.40 in. (Over 30 to 35 mm) | 1.05 |
| Over 1.40 to 1.60 in. (Over 35 to 40 mm) | 1.04 |
| Over 1.60 to 1.80 in. (Over 40 to 45 mm) | 1.03 |
| Over 1.80 to 2.00 in. (Over 45 to 50 mm) | 1.02 |
| Over 2.00 to 2.40 in. (Over 50 to 60 mm) | 1.01 |
| Over 2.40 to 3.20 in. (Over 60 to 80 mm) | 1.00 |
| Over 3.20 to 3.40 in. (Over 80 to 85 mm) | 0.96 |
| All pavement with a profile index (PI0.0) greater than 3.40 in. (85 mm) shall be corrected to 3.40 in. (85 mm). |