PCCP SMOOTHNESS

The Standard Specifications are revised as follows:

SECTION 501, DELETE LINES 571 THROUGH 571aa.

SECTION 501, AFTER LINE 572, INSERT AS FOLLOWS:

| SECTION PAY FACTORS FOR SMOOTHNESS (PI0.0) ZERO BLANKING BAND |
| --- |
| Design Speed Greater Than 45 mph (70 km/hr) |
| Profile Index in./0.1 mi. (mm/0.16 km) | Pay Factor |
| Over 0.00 to 1.40 in. (Over 0 to 35 mm) | 1.06 |
| Over 1.40 to 1.60 in. (Over 35 to 40 mm) | 1.05 |
| Over 1.60 to 1.80 in. (Over 40 to 45 mm) | 1.04 |
| Over 1.80 to 2.00 in. (Over 45 to 50 mm) | 1.03 |
| Over 2.00 to 2.40 in. (Over 50 to 60 mm) | 1.02 |
| Over 2.40 to 2.80 in. (Over 60 to 70 mm) | 1.01 |
| Over 2.80 to 3.60 in. (Over 70 to 90 mm) | 1.00 |
| Over 3.60 to 3.80 in. (Over 90 to 95 mm) | 0.96 |
| All pavements with a Profile Index (PI0.0) greater than 3.80 in. (95 mm) shall be corrected to 3.80 in. (95mm). |