QC/QA PCCP AIR CONTENT

The Standard Specifications are revised as follows:

SECTION 501, BEGIN LINE 522, DELETE AND INSERT AS FOLLOWS:

(b) Air Content

When test results for air content exceed the allowable tolerance or range, a pay factor will be assessed as follows:

1. Lots

| Lot Average Air Content |
| --- |
| Percent % | Pay Factors |
| > 10.0 9.9 | * |
| 10.0 9.7 – 9.8 | 0.80 |
| 9.7 – 9.9 | 0.85 |
| 9.5 – 9.6 | 0.91 0.90 |
| 9.3 – 9.4 | 0.96 0.95 |
| 9.0 – 9.2 | 0.98 0.99 |
| 5.7 – 8.9 | 1.00 |
| 5.0 – 5.6 | 0.99 0.93 |
| 4.7 – 4.9 | 0.98 |
| 4.6 5.5 | 0.88 0.90 |
| 4.5 5.4 | 0.80 0.85 |
| < 4.5 5.3 | * 0.79 |
| <5.3 | * |

*	The PCCP will be adjudicated as a failed material in accordance with normal Department practice as listed in 105.03. The PCCP may be subject to removal and replacement or left in place with reduced or no payment.

| Lot Range for Air Content |
| --- |
| Percent % | Pay Factors |
| 0.0 – 2.5 | 1.00 |
| 2.6 – 3.0 | 0.99 |
| 3.1 – 3.5 | 0.97 |
| > 3.5 | * |

*	The PCCP will be adjudicated as a failed material in accordance with normal Department practice as listed in 105.03. The PCCP may be subject to removal and replacement or left in place with reduced or no payment.

2. Sublots

If a sublot value is less than 4.0 5.0% or greater than 10.0%, the PCCP will be adjudicated as a failed material in accordance with normal Department practice in accordance with 105.03. For a sublot completely removed, the sublot test value from the replacement sublot will replace the original test value.