WOOD CONDITIONING

The Standard Specifications are revised as follows:

SECTION 911, BEGIN LINE 395, DELETE AND INSERT AS FOLLOWS:

TABLE E

| CONDITIONING METHODS PERMITTED AND TEMPERATURE REQUIREMENTS FOR METHOD USED |
| --- |
|  | HEATING IN |
|  | STEAMING | PRESERVATIVE |
| SPECIES | CONDITIONING METHODS PERMITTED | Max. Temp °F (°C) | Max. Duration Hrs. | Max. Temp °F (°C) | Max. Duration Hrs. |
| Hard Maple | Air drying only |  |  |  |  |
| Other Hardwoods(1) | No Steaming |  |  | 220 (104) | No Limit |
| Southern Pine | Shown in 910.02(f)5i All | 245 (118) | 17 | 220 (104) | No Limit |
| Eastern White Pine | All | 240 (116) | 4 1/2 | 210 (99) | 6 (3) |
| Other Softwoods(2) | Shown in 910.02(f)5i All | 240 (116) | 6 | 210 (99) | 6 (3) |

(1)	Red Oak, White Ash, White-heartwood beech, Yellow Birch, Hickory, and Red Maple

(2)	Jack Pine, Douglas Fir, and Red Pine

(3)	If seasoned material is used, otherwise, no limits