GEOTEXTILE MATERIAL PROPERTIES

The Standard Specifications are revised as follows:

SECTION 918, BEGIN LINE 22h, DELETE AS FOLLOWS:

GEOTEXTILE MATERIAL PROPERTIES

| TEST | METHOD | REQUIREMENTS* |
| --- | --- | --- |
| Tensile Strength | Grab Tensile Strength, ASTM D 4632 | 200 lb (890 N) |
| Elongation | Grab Tensile Strength, ASTM D 4632 | 15% |
| Seam Strength | Grab Tensile Strength, ASTM D 4632 | 180 lb (800 N) |
| Bursting Strength | Mullen Burst, ASTM D 3786 | 320 psi (2.21 MPa) |
| Puncture Strength | ASTM D 4833 | 80 lb (356 N) |
| Trapezoid Tear | ASTM C 4533 | 50 lb (225 N) |
| Ultraviolet Degradation at 150 h | ASTM D 4355 | 70% strength retained |
| Apparent Opening Size (AOS) | ASTM D 4751 | AOS shall be No. 50 (300 µm) standard sieve or filter |
| Permeability** | ASTM D 4491 (Permittivity) | 0.01 cm/sec or > |

*	Use value in weaker principal direction. All numerical values represent minimum average roll value and test results from any sampled roll in a lot shall meet or exceed the minimum values in the table. Lots shall be sampled according to ASTM D 4354.

**	The nominal coefficient of permeability shall be determined by multiplying permittivity value by nominal thickness. The nominal thickness is measured under a normal load of 280 psi (1.93 MPa).

SECTION 918, BEGIN LINE 52, DELETE AS FOLLOWS:

The geotextile shall be in accordance with the physical requirements as follows.

| TEST | METHOD | REQUIREMENTS2 |
| --- | --- | --- |
| Grab Strength | ASTM D 4632 | 80 lb (355.8 N) |
| Seam Strength1 | ASTM D 4632 | 70 lb (311.4 N) |
| Puncture Strength | ASTM D 4833 | 25 lb (111.2 N) |
| Burst Strength | ASTM D 3786 | 130 psi (896 kPa) |
| Trapezoid Tear | ASTM D 4533 | 25 lb (111.2 kg) |
| Apparent Opening Size (AOS) | ASTM D 4751 | Sieve No. 50 or smaller opening |
| Permeability | ASTM D 4491 | 0.1 mm/sec |
| Ultraviolet Degradation at 150 h | ASTM D 4355 | 70% strength retained |

1	Values will apply to both filed and manufactured seams.

2	The value in the weaker principal direction shall be used. All numerical values will represent the minimum average roll value. Test results from a sampled roll in a lot shall be in accordance with or shall exceed the minimum values shown in the table. Lots shall be sampled in accordance with ASTM D 4354.