HIGH MAST POLES

The Standard Specifications are revised as follows:

SECTION 920, BEGIN LINE 213, DELETE AND INSERT AS FOLLOWS:

1. High Mast Poles

The poles shall be made of steel in accordance with ASTM A 560, grade C 871 (A 871M). The steel shall have a minimum yield strength of 59,500 psi (410 MPa).