HIGH RANGE WATER REDUCERS

IN PRECAST PRESTRESSED CONCRETE STRUCTURAL MEMBERS

The Standard Specfications are revised as follows:

SECTION 707, BEGIN LINE 121, DELETE AND INSERT AS FOLLOWS:

(c) Concrete. Concrete shall be air entrained and in accordance with the

applicable provisions requirements of 702.05. Water-reducing, or water-reducing and retarding

admixtures, or approved high range water reducing portland cement concrete admixture systems may be used. Air entraining agents, type A, and type D admixtures shall be certified in accordance with 912.03(c). HRWR systems shall be certified in accordance with 912.02(e). The use of either a type A or a type D chemical admixture shall be in accordance with 702.05 as specified for class C concrete. If a high range water reducing admixture system is to be used in portland cement concrete, the procedures for batching shall be consistent. The concrete shall be mixed until a uniform consistency is achieved.

Admixtures shall not contain chlorides which have been added

SECTION 707, LINE 128, INSERT AS FOLLOWS:

will not apply. Slump shall be no less than 50 mm (2 in.) nor more than 125 mm (5 in.). Concrete with high range water reducing admixtures shall be in accordance with the requirements as follows:

1.	The slump shall be a minimum of 75 mm (3 in.) and a maximum of 150 mm (6 in.).

2.	The amount of time from mixing to final placement and consolidation shall be a maximum of 30 minutes.

3.	The concrete mixture shall not be retempered with additional amounts of high range water reducing admixture after the initial mixing has been completed.

SECTION 912, AFTER LINE 58, AND INSERT AS FOLLOWS:

6. Type F. Type F is a high range water reducing admixture that reduces the quantity of mixing water required to produce concrete of a given consistency and retards the setting of concrete.

7. Type G. Type G is a high range water reducing and retarding admixture that reduces the quantity of mixing water required to produce concrete of a given consistency by 12 percent or greater and retards the setting of concrete.

SECTION 912, BEGIN LINE 86, DELETE AND INSERT AS FOLLOWS:

2.	For all other Type A, B, C, D, and E admixtures, the certification shall:

SECTION 912, AFTER LINE 103, DELETE AND INSERT AS FOLLOWS:

3.	For high range water reducing and high range water reducing and retarding admixtures the certification shall state:

a.	The product name.

b.	The manufacturer's name.

c.	The character of the material.

d.	That there has been no change in raw materials, formulation, or procedure since the department's evaluation of this product.

e.	The chloride content.

f.	Whether or not chloride is added as an ingredient of manufacture.

g.	The admixture is in accordance with AASHTO M 194, Type F or Type G.

3 4.	The test shall be performed by a recognized laboratory which is a state

SECTION 912, AFTER LINE 134, INSERT AS FOLLOWS:

(e) Approved High Range Water Reducing Systems. The Department will maintain a list of HRWR systems that have met requirements for approval.

(e f) Performance of Admixtures. The use of concrete admixtures which

444444444444444444444444444444444444444444444444444444444444444444444444