UNIFORM RIPRAP

The Standard Specifications are revised as follows:

SECTION 904, BEGIN LINE 694, INSERT AS FOLLOWS:

(d) Uniform Riprap. The material shall be coarse aggregate, Class F or higher in accordance with 904.03(a). Gradation shall be in accordance with 904.04(e). Either type A or type B may be utilized.

(e) Sizes of Riprap.

| GRADATION REQUIREMENTS |
| --- |
| Percent Smaller |
| Size, mm (in.) | Revetment | Class 1 | Class 2 | Uniform A | Uniform B |
| 750 (30) |  |  | 100 |  |  |
| 600 (24) |  | 100 | 85-100 |  |  |
| 450 (18) | 100 | 85-100 | 60-80 |  |  |
| 300 (12) | 90-100 | 35-50 | 20-40 |  |  |
| 200 (8) |  |  |  | 100 |  |
| 150 (6) | 20-40 | 10-30 | 0-20 | 35-80 | 95-100 |
| 75 (3) | 0-10 | 0-10 | 0-10 |  | 35-80 |
| 25 (1) |  |  |  | 0-20 | 0-20 |
| Depth of Riprap, minimum | 450 mm (18 in.) | 600 mm (24 in.) | 750 mm (30 in.) |  |  |